## Slide 1: Extension of plasma torch operation with reactive gases for wall cleaning purposes
E.R. Ionita, C. Stancu, T. Acsente, M. Teodorescu, G. Dinescu
National Institute for Laser, Plasma and Radiation Physics, Atomistilor 409, PO-Box MG-16, 077125, Magurele, Bucharest, Romania

## Slide 2: Task: WP10-PWI-02-04-01/MEdC/BS
Objectives:
1. Investigation of device operation with reactive gases (January-June 2010)
  Manufacturing of new constructive elements of the plasma torch, suitable to work in reactive gases; improvement of flexibility;
  Study of the influence of reactive gases (nitrogen, air, others) on the operation domain, lifetime and stability;
2. Experiments of cleaning with plasma torch working in nitrogen/argon/reactive gases (July-December 2010);
  Cleaning of carbon layers laboratory coated flat and castellated surfaces;
  Cleaning of mixed layers from laboratory or Tokamak exposed surfaces.

## Slide 3
Cleaning with plasma torch
- stainless steel body;
- hand held, flexibility for mounting on robotic arm;
- couplings realized to the back end: RF power, gas feeding, active water cooling (2 circuits, inside the RF electrode and external jacket)
Plasma torch
Inside gap cleaning
Removal conditions
Nitrogen flow = 8200 sccm
RF power = 350 W
Distance from top face of the built castellation = 2mm
Scanning speed = 5mm/s
Gap width = 0.5 – 1.5 mm

## Slide 4
Inside gap cleaning

## Slide 5
PLASMA TORCH REMOVAL OF a-C:H LAYERS (FLAT)
Layer thickness: 1 m
Number of scans: 1
Power: 350 W
Nitrogen, mass flow rate: 7500 sccm
Layer thickness: 2 m
1.66 mm/sec
1.66 mm/sec
5 mm/sec

## Slide 6
Effect of torch-gap relative position on cleaning
1 scan 46 scans 101 scans
Torch on the middle of gap
Torch on the side of the gap
1 scan 20 scans 50 scans

## Slide 7: Local and integral cleaning rates
The profiles of the thickness of the inside gaps uncleaned layer after 46 et 100 scans
Dependence of the local cleaning rates upon gap depth
,
Conclusions:
-The removal of a-C:H layers from the inside of gaps with width of 0.5-1.5 mm was demonstrated;
- The rates are higher for narrow gaps;
-The rates are higher at the top part (entrance) of the gaps
-Torch over the gap middle
- Nitrogen flow rate 8200 sccm,
-RF power 350 W
-Distance to surface 2mm
-Scan speed 5mm/s
-Gap width: 0.5 mm

## Slide 8: Improvement for working with reactive gases
- Possible higher removal rates can be obtained by using reactive gases, oxygen, air, ammonia, hydrogen or their mixtures;
- Working with reactive gases may lead shortage of the device lifetime, limited domains of operation;
To be taken into consideration:
Electrodes oxidation: i) new materials resistant to oxidation, ii) keep the electrodes cold;
Wider range of plasma impedance with various gases: research on matching, firmer connections, high quality cables;
Instability of operation: research on operation domains, discharge stability in various gases.

## Slide 9: Changes on RF electrode materials and manufacturing
Brass replaced thoroughly with stainless steel material for RF electrode
Diameter of the active RF electrode increased from 8 mm to 10 mm
Gas admission changed from internal part of the RF electrode, to the outer of the RF electrode;
Direct connection of the RF cable, use of RF- 7/16 connector avoided.
Changes on the cooling inside the internal RF electrode
Replace Polyethylene Terephthalate (PET) tubes with Fluorinated Ethylene Propylene (FEP) tubes (resistant to temperature, shriveling and plying );
Increase the water volume in RF electrode from 2.3 cm³ to 3.4 cm³ ;
Increase water inlet and outlet inner diameter, from 1 mm to 1.8 mm;
Water flow rate increased from 0.6 to 1.5 liter/ min.
Work performed

## Slide 10: Final Assembly
Conclusions:
-more robust;
-more compact and flexible, easier to be integrated on a robotic arm;
-increased cooling;
-reliable RF connection;
-more resistant on corosion;
Outer jacket
Internal Electrode
Gas admission tube
Cooling tubes
Pass-through RF line
& ground connection

## Slide 11: Study of operation in reactive gases
Pure gases
- Argon: Ar
- Nitrogen: N2
- Oxygen: O2
Mixtures
- Air
- Argon/Ammonia: Ar/NH3:
- Argon/Hydrogen: Ar/H2
- Argon/Oxygen
List of used gases

## Slide 12: Aim: torch operation in reactive gases
Criteria:
Plasma jet visible (expansion outside the interelectrodic space)
Stable operation without spots and arcing;
No excessive heating (returning cooling water still cold, no visible reddish on nozzle)
Operation domains: power and flow rate measurements
Jet appearance: imaging
Cleaning example
Establish the possible values for the power (P), gas flow rate values (), and gas flow rate ratios for stable and reliable operation

## Slide 13: Operation domains in pure gases
Conclusions
Operation in nitrogen and air require more power;
Operation in air: domain in air restricted to a smaller area
Best operation points in the middle of the operating domains (Ar: 5000-6000sccm, 150-200W)

## Slide 14
Operation domains in gas mixtures
Conclusions
Operation in Ar/O2 requires more power;
Operation in ammonia is the easiest;
Operation points should be chosen in the middle of the operating domains (Ar: 5000 sccm, admixed gas 500-1500 sccm, powers 200-300 W).

## Slide 15
Operation domains in pure gases: imaging
Ar, 140W
4000sccm Ar 6000sccm Ar 8000sccm Ar
N2, 300W
4000sccm N2 6000sccm N2 8000sccm N2
2000sccm 3000sccm 4000sccm
O2 350W
2000sccm 3000sccm 4000sccm
Air 300W

## Slide 16
100sccm H2 300sccm H2 500sccm H2
160W 5000sccm Ar, H2 variable
100sccm NH3 200sccm NH3 500sccm NH3
130W: 5000sccm Ar, NH3 variable
Operation domains in gas mixtures: imaging
300W, 5000sccm Ar, O2 variable
O2 100sccm O2 200sccm O2 300sccm

## Slide 17
Preliminary results on cleaning with reactive gases
300W 5000sccm Ar+20sccm O2
300W 5000sccm Ar+200sccm H2
300W 5000sccm Ar+500sccm NH3
350W 5000sccm N2
300W 4000sccm Air
300W 3000sccm O2
after 1 scan, speed 5 mm/sec, distance to nozzle 5 mm
Effectiveness: O2 >>Ar/O2>>Air~N2>>Ar/H2>>Ar/NH3

## Slide 18: Encountered problems
In pure O2 or large O2 content (over 10%) and air :
- Long time operation not proved
- The nozzle does not resist for long time in oxygen – should be changed in Mo or W material
- The insulator (quartz) is eroded fast – other material or change of design
Alternative solution: Reactive gas injection in the nozzle or even in post-discharge

## Slide 19
Conclusions and further work
- Experiments of cleaning with plasma torch working in nitrogen/argon/reactive gases (July-December 2010);
  - Cleaning of carbon layers from laboratory coated flat and castellated surfaces;
  - Cleaning of mixed layers from laboratory or Tokamak exposed surfaces.
- The torch works well in Ar, N2, Ar/NH3, Ar/H2 gases
- Still problems with oxygen containing gases, at large admixed %
- The best cleaning results are in oxygen, Ar/O2, air, nitrogen
Further work:

## Slide 20
Thank you for your time !