## Slide 1
Stimulated
Raman Scattering
Coherent
anti-Stokes Raman Scattering

## Slide 2
A. Surface Enhanced Raman Scattering (SERS) as
nonlinear optical effect.
B. New features of the Raman spectra of single-walled
carbon nanotubes highly separated into
semiconducting (99%) and metallic (98%) components.
I.Baltog, M.Baibarac, L.Mihut,

## Slide 3
Outline
A • Background of Raman light scattering
• Methods of amplification of the Raman emission
• Surface Enhanced Raman Scattering (SERS) via plasmons excitation
• SERS mechanism as a nonlinear optical process.
B• Brief introductions in the Raman spectroscopy of carbon nanotubes
• Abnormal Anti-Stokes SERS spectra of single-walled carbon nanotubes as
single beam CARS effect .
• Anti-Stokes and Stokes SERS spectra of single-walled carbon nanotubes
highly separated into semiconducting (99%) and metallic (98%) nanotube
components.
C • Summary

## Slide 4
v3
v2
v1
v0
v3
v2
v1
v0
Excitation
Excitation
Excitation
Excitation
Raman Stokes
Raman Stokes
Raman anti-Stokes
Raman anti-Stokes
Virtual levels Electronic levels

## Slide 5
Raman light scattering is an complex interaction of photons
and intrinsic molecular bonds
E = E0cos2lt incident electromagnetic wave (laser beam)
P = E =  E0cos2lt induced electric dipole moment ;  is the polarizability
4 classical expression of total scattered light
 = o + + …  is polarizability that changes by molecular vibration; Q is coordinate that describes molecular
vibration
P = E = o E0cos2lt + E0 0 [cos2(l + )t + cos2(l - )t ]
Rayleigh
scattering
Anti-Stokes Stokes
Raman scattering
Both branches are amplified equally
with the excitation light intensity
I(l) >> IS >> IaS
1 >> 10-6 >> 10-9
Intensity
Values at
~ 1500 cm-1

## Slide 6
Characteristic Raman
frequencies
PbI2 ; ZnO ; CCl4 ; TiO2
C60; SWNTs; graphene
Changes in frequency
of Raman peak
Chemical interaction;
stress; strain; temperature
Polarization
of Raman peak
Crystal symmetry ;
orientation; antenna effect.
Width
of Raman peak
Morphology: crystal;
mesoscopic and nanometric
structures;
Intensity
of Raman peak
 Amount of material;
film thickness;
 Nonlinear optical
effects
Information from Raman spectroscopy
║
┴

## Slide 7
B.C
676.4 nm
514.5 nm
B.V
ωp
ωS
ħω1
ωaS = 2ωP – ωS
kaS =2kP -kS
ħ(2ωP – ωS)
ωp-ωS=Ω
k(ω0)
k(ω0)
k(ω1)
k(2ω0-ω1)
x 104
x104 -106
x104-108
x104-1010
Methods of amplification of the Raman emission
Resonant excitation
SERS effect
chemical + plasmons
Stimulated Raman effect
CARS effect
SERS
chemical
SERS
plasmons
SERS plasmons

## Slide 8
Abnormal anti-Stokes SERS spectra of CuPc under resonant
excitation
exc = 647.1 nm is resonant for CuPc
1
2
1
2

## Slide 9
J.L.Coutaz et al. Phys Rev B,32,227,(1985)
Second harmonic
generation
Stimulated Raman
effect
I.Baltog et al. J.Opt.Soc.Am.,13, 656,(1996)
C.Steuwe, et al. Nano Lett. , 11, 5339;(2011)
RL Aggarwal ; et al. Appl. Spectrosc.. 67 ,
132-135 ,(2013)
CARS effect
 Single beam :
I.Baltog et al. Phys. Rev. B,72,(24), 245402,(2005)
J.Appl.Phys,110, 053106,(2011)
 Double beams
Surface plasmons as a channel to generate by optical
pumping non-linear effects.
IL >> IS ωL +  ☛ CARS
ω = ωL± (ωL – ωS) =
ωS ☛ Stimulated
Raman

## Slide 10
Second harmonic
generation
Stimulated Raman
effect

## Slide 11
p-polarization: E-field is parallel to the plane of incidence
s-polarization: E-field is perpendicular to the plane of incidence (German senkrecht = perpedicular)
x
z
y
q1
Hx
q2
z=0
e1
e2
Ey
H
Hz
x
z
y
q1
Ex
Ez
q2
z=0
e1
e2
Hy
E
Any linearly polarized radiation can be represented as a superposition of p - and s - polarization.

## Slide 12
x
z
y
z=0
e1
e2
E1x
E1z
H1y
E1
p-polarized incident radiation will
create polarization of charges at
he interface.
These charges give rise to a surface plasmon modes
E2x
E2z
H2y
E2
creation of the polarization charges
if one of the materials is metal, the electrons will respond to this polarization. This will give rise to surface plasmon modes
Boundary condition: (a) transverse component of E is conserved,
(b) normal component of D is conserved

## Slide 13
x
z
y
z=0
e1
e2
H1x
H1z
E1y
H1
s-polarized incident radiation does not create polarization charges at the interface. It thus can not excite surface plasmon modes
H2x
H2z
E2y
H2
no polarization charges are created  no surface plasmon modes are excited!
Boundary condition (note that E-field has a transverse component only):
transverse component of E is conserved,

## Slide 14
Maxwell’s equations
Charge neutrality,  = 0
No direct current, j = 0 Non-magnetic materials, r = 1 ( = 0)
dielectric 1
metal 2
localized surface mode = surface plasmon
decaying into both materials
wave propagating in x-direction
z
x
y
E1z
E1x
E1
intensity
condition imposed on k-vector
Surface Enhanced Raman Scattering
(SERS)
via plasmons excitation

## Slide 15
Caracteristicile undelor de suprafata = plasmoni de suprafata (SP) :
undele de suprafata rezulta din oscilatiile colective ale electronilor din stratul metalic ; pot fi excitate numai cu radiatie cu polarizata p (TM), care are o componenta EM perpendiculara la suprafata
undele de suprafata sunt propagative in lungul suprafetei de separare dintre doua medii (metal-dielectric) aflate in contact;
pentru λexc = 500 nm; Lpropagare≈ 25 μm
(ii) unde evanescente pentru care amplitudinea scade exponential cu distanta de la suprafata de separare –
pentru : λexc = 500 nm; hpenetrare ≈ 12 nm in metal si ≈ 95 nm in aer
amplitudinea undei evanescente este maxima in lungul suprafetei lor de separare
(iv) Metale active Pb, In, Hg, Sn, Cd  UV si Cu, Au, Ag  VIS

## Slide 16
metal
coupling gap
prism
q1
Otto geometry
metal
prism
q1
Kretschmann-Raether
geometry
Grating
METHODS OF PLASMON EXCITATION
 rough surface 
dielectric e1
metall e2

## Slide 17
Experimental
Material:
- copper-phthalocyanine (CuPc)
- SWNTs highly separated in semiconducting (99%) and metallic (98%)
components
Sample form :
- thin films (9.5; 39; 88; 185 nm thickness ) deposited on glass and
rough Au and Ag supports with different SERS activity;
motivation: SERS(Au) << SERS(Ag)
Measuring geometry : Backscattering under focused light ; x50 aperture objective
Excitation laser light : 514.5 ; 647.1;676.4 nm ensuring non-resonant and
resonant optical excitation

## Slide 18
Abnormal anti-Stokes SERS spectra of CuPc under resonant
excitation
exc = 647.1 nm is resonant for CuPc
1
2
1
2

## Slide 19
SERS spectroscopic studies on CuPc thin films under
non-resonant ( 514.5 nm) and resonant (647.1 nm) optical excitation.
Anti-Stokes and Stokes Raman spectra of CuPc thin
Films of 39 nm thickness deposited on Ag, Au and
glass supports. Red curves show the anti-Stokes spectra
calculated with the Boltzmann formulae applied to the
corresponding Stokes Raman spectra.
Anti-Stokes and Stokes Raman spectra of CuPc thin
Films of 39 nm thickness deposited on Ag, Au and
glass supports. Red curves show the anti-Stokes
spectra calculated with the Boltzmann formulae
applied to the corresponding Stokes
Raman spectra.
SRS
CARS

## Slide 20
Intensities of the anti-Stokes and Stokes Raman lines
at 1530 cm-1 of 39-nm-thick CuPc films deposited on
glass, Au and Ag supports. Raman measurements were
performed in a backscattering geometry under non-resonant (514.5 nm) and resonant (647.1 nm) optical excitations.
Data were all obtained at the same laser intensity (2 mw)
focused by a 50x objective onto the surface sample.
Data for each Raman branch were normalized to the
intensity measured on the film deposited on a
glass support.
I(L) >> I(S) >> I(aS)
1 10-6 10-9
SP(L) >> SP(S) >> SP(aS)
SP(L)  SP(S) = SRS
I(L) >> I(S) ≈ I(aS)
1 10-6 10-6
SP(L) >> SP(S) > SP(aS)
SP(L)  SP(S) SRS
(2SP(L) ± SP(S))  SP(aS) CARS
SRS
for a Raman line at ~1500 cm-1

## Slide 21
Diagrams of variations of the anti-Stokes
and Stokes Raman line at 1530 cm-1 of
CuPc at different excitation wavelength
( non-resonant : 514.5 and resonant :
647.1 nm), film thickness (9.5, 39 and 88 nm)
and substrates used glass, Au and Ag.
Intensities one each branch were normalized
to the value measured on glass substrate.

## Slide 22
Intensity of the anti-Stokes and Stokes Raman line at
1560 cm-1 of CuPc thin films of 9.5 nm thickness
deposited on glass, Au and Ag supports under
non-resonant (514.5 nm) and resonant (647.1 nm)
laser excitation.Data were normalized to the intensity
obtained on glass support.
I(L) >> I(S) ≈ I(aS)
1 10-6 10-6
SP(L) >> SP(S) ≈ SP(aS)
SRS
SP(L)  SP(S)
CARS
(2SP(L) ± SP(S))  SP(aS)
Film thickness matched by plasmons wave penetration depth
A2

## Slide 23
 SERS mechanism can be considered a nonlinear optical process ?
Yes, this is demonstrated by the deviations from the Boltzmann law.
<
I(l) > I(S) > I(aS)
SPs(l) > SPs(S) > SPs(aS)
mixing of surface waves (SW)
SW(1) + SW(S) + SW(aS)
lower frequencies are amplified at the expense of the higher frequencies
Stimulated Stokes Raman effect (SRS)
higher frequencies are amplified at the expense of the lower frequencies
Coherent anti-Stokes Raman effect (CARS)
Plasmons coupling mechanism
CARS
SRS
ωmix = ωL± (ωL – ωs)
ωmix = ωL- (ωL – ωs) = ωs
ωmix = ωL+ (ωL – ωs) = 2ωL- ωS = ωL+ Ω = ωaS

## Slide 24
Carbon allotropic particles
Graphite
Diamond
Fullerene : C60
Graphene
Single wall carbon nanotubes
Multi-wall carbon
nanotubes
metallic
semiconductor

## Slide 25
Carbon nanoparticles |  |  |  | 
1996 Nobel prize Chemistry | Robert F. Curl Jr., Harold W. Kroto, Richard E. Smalley | Fullerene |  | 
2008 Inaugural Kavli Prize for Nanoscience | Sumio Iijima | Carbon nanotubes |  | exc = 647.4 nm exc = 514.5 nm
2011 Nobel prize Physics | Andre Geim, Konstantin Novoselov | Graphene |  | exc = 457.9 nm

## Slide 26
d = Ch / π = 31/2aC-C(m2 + mn + n2)1/2/ π
= tan-1[31/2m/(m+2n)]
N(hex/u.c) = 2(m2 + mn + n2)/d
(n,m) denote the number of unit vectors na1 si ma2
in the hexagonal honeycomb lattice contained in the
vector Ch
 chiral angle
aC-C = 1.421 Ǻ is the nearest-neighbor C-C distance in graphite
n,m, define a specific SWNT:
► Armchair (n = m, =300 ),
► Achiral or zig-zag (n ≠ 0 or m = 0 ;  = 00 )
► chiral (n ≠ m ≠ 0 ; 00< <300 ).
for n-m = 3k , k = 1,2,3.. Metallic properties
for n-m ≠ 3k Semiconducting properties
Geometry of single-walled carbon nanotube (SWNT)
 = 00 ;  = 300 ; 0<<300

## Slide 27
Electronic structure
- SWNT has one-dimensional (1D) electronic density of states
1D electronic band structure derive from the 2D band structure
of the graphene honeycom sheet.

## Slide 28
► The structure of electronic bands density of an one dimensional system (1D- carbon nanotube) derives from
the bi dimensional structure (2D) of graphite
► A set of 1D energy dispersion relations is obtained by slicing up the 2D energy band structure of graphite in the
circumferential direction.
where a = 1.42 x Ǻ =2.46 Ǻ is lattice constant of two dimensional graphite kx and ky are the corresponding basis vectors of the reciprocal lattice; γ0 is nearest-neighbor transfer integral
For an armchair SWNT tube the 1D energy dispersion relation is:
(-π < ka < π ); m = 1,.....,5 ;
Similarly for a zig-zac SWNT tube:
m = 1,.....,9 ;
k is one dimensional vector along the tub axis
► The calculations for the electronic structure of SWNTs show that about 1/3 of the nanotubes are metallic and 2/3
are semiconducting , depending on the nanotube diameter dt and chiral angle θ.
►The metallic SWNT have a small non-vanishing 1D density of states at the Fermi level while for the semiconducting
1D SWNT the density of states is zero.
► The band gap for isolated semiconducting carbon nanotubes is proportional to the reciprocal nanotube diameter 1/dt

## Slide 29
The tubes diameter and calculated band gap energies as function of n,m,  parameters .
Absorption spectrum of SWNT
514.5 nm
2.4 eV
676 nm
1.83 eV
1064 nm
1.16 eV

## Slide 30
Electronic structure
Electronic 1D density of states for two (n,0) zig-zag nanotubes.Dotted line shows the density of states for the 2D graphene sheet
(R.Saito,M.S Dresselhaus et al J.Appl.Phys 73,494,(1993))
radial breathing modes RBM
RBM (cm-1) = α/d (nm ) ;
223.75<α<248
transversal axial
-longituginal

## Slide 31
Stokes and anti-Stokes SERS spectra
on SWNTs films of different thicknesses
(h1<h2<h3, i.e about 30, 60 and 120nm )
recorded through a microscope objective
of x0.55 numerical aperture under
excitation wavelengths
of 676.4 and 514.5 nm.
The IaS/IS ratio was estimated for
the G band. Au as metallic SERS support
Explanation:
Single beam CARS effect
SERS spectra of mixture semiconductor (66%) and metallic (33%)
carbon nanotubes packed in bundles
I.Baltog et al .Phys Rev B,72,(24), 245402,(2005)  SWCNTs
J. Raman Spectrosc,42,303,(2011)  conducting polymers
J. Appl. Phys., 110, 053106, (2011)  nonlinear optical materials

## Slide 32
Abnormal anti-Stokes Raman scattering under resonant optical excitation
of SWNTs is a process reminiscent to a single beam CARS effect.
ICARS ~ NA ωaS2d2 |χ(3)|2 I2l.IS sinc2(|Δk|.d/2)
where : Il - incident pump intensity;
χ(3) - the dielectric susceptibility; d - slab thickness; Δk - the phase-mismatch requirement  (Δk = kas – (2 kI– kS) ; kas, kS ,kI are the wave vectors); NA is the numerical aperture of the
collecting lens.
weak temperature
dependence
Baltog et all. Journal of Optics A: Pure and Applied Optics 7, 1-8, (2005) ;
Phys Rev B,72,(24), 245402-245413,(2005) ;
a-Stokes
Stokes

## Slide 33
B. Anti-Stokes and Stokes SERS spectra of single-walled
carbon nanotubes highly separated into semiconducting (99%) and metallic (98%) nanotube components.
Calculated Kataura plots of
van Hove singularities
Energy vs. tub diameter
B1. Absorption spectra of semiconducting (99%) and metallic (98%) SWNT
676
514

## Slide 34
Fano asymmetry
●The quantum interference between two configurations in the transition process into a final state with the same energy:
one direct <2‌α2|0> and one indirect via a discrete state <2‌W|1> <1‌α1|0> , where W is a matrix element describing a nonradiative transition from discrete to continuum.
●The energy continuum of these transitions overlaps with the energy of the discrete Raman active optical phonon of the same symmetry and an interference between the phonon and the electronic transition takes place.
Breit-Wigner-Fano (B WF) profile :
I=I0{1+(0 - )/}2/{1+[(0 - )/]2}
 = line width ;
 = parametre of asymetery
M.A.Pimenta, …,G.Dresselhaus, and M.S.Dresselhaus.., Phys.Rev.B 58,R16016-R16019,(1998)

## Slide 35
Stokes and anti-Stokes Raman spectra for SWNT’s of d~1.49 nm taken at four different values of E laser
S. D. M. Brown et al. Phys. Rev. B 61, R5137(2000)
TO
TO
LO
LO
Raman G+ and G- peaks associated to LO and TO
phonons for semiconducting and metallic SWNTs
S. Piscanec et al. Phys. Rev. B 75, 035427(2007)
?

## Slide 36
 Since metals are infinitely polarizable, it is hard to see how a vibration of the atoms
in the crystal lattice could cause a change in the polarizability.
Raman activity of metals may be generated by small clusters of metal atoms, and in
the case of metallic nanotubes by their association in bundles
 Fano Raman profile
The relative BWF intensity is always weak for thin
bundles or individual tubes but varies for thicker
bundles. The solid lines show estimated relative intensities
for pure metallic bundles and bundles containing isolated
or noninteracting metallic tubes.
K.Kempa et al. Phys Rev B 66, 161404 (2002);
66, 195406 (2002)

## Slide 37
Anti-Stokes (a1;b1) and Stokes (a2;b2) G Raman band profiles of metallic (~98% pure, a1;a2) and semiconductor (~99% pure, b1;b2) SWNTS deposited in a thin layer on glass (black), Au (red) and Ag (blue) supports. All spectra were recorded in a backscattering geometry with 2 mW of laser intensity focused on the sample through a 50x objective.
Supports:  glass ;  Au;  Ag
G Raman band profiles of metallic ( 98%) and semiconductor (99%)
carbon nanotubes

## Slide 38
Intensities of the anti-Stokes and Stokes G Raman lines (1595 cm-1) under 514.5; 647.1 and 676.4 nm excitation light (normalized by the intensity obtained from samples with the glass substrate) for metallic (M, ~98 % pure) and semiconductor (S, ~99% pure) C-SWNT thin films deposited on glass, Au and Ag supports. The intensity of the laser light focused on all samples was 2 mW.
SERS evidence of anomalous behavior in anti-Stokes Raman branch
of metallic nanotubes.
Stimulated
Raman
Scattering
effect
CARS effect

## Slide 39
MWNT
LAUSANNE
Metallic
MWNT
ALDRICH
Metallic +
Semiconductor
Supports:
 glass
 Au
 Ag

## Slide 40
EF
Conduction
band
Valence
band
Conduction
band
Vibration
levels
Eg
Energy
METAL
INSULATOR or
SEMICONDUCTOR
Insulator, semiconductor and metal
Clasification based on bandstructure

## Slide 41: Absorption: Semiconductors
• Absorption by electron transition occurs if hn > Egap
incident photon energy hn
Energy of electron
filled states
unfilled states
I
o
typical resonance
Egap

## Slide 42: Optical Properties of Metals: Absorption
• Absorption of photons by electron transition:
• Metals have a fine succession of energy states that causes absorption and reflection;
• Normally, the Raman activity is conditioned of the vibrations which change the
poalarizability of the molecule or material.
• Because the visible light cannot penetrate the metals , Raman scattering results from
the modulation of the electronic susceptibility by the optical vibration modes within
the skin depth by the optical vibration modes .
• Inside the medium, the amplitude of the electric field decays to zero rapidly with
distance.
Energy of electron
Incident photon
filled states
unfilled states
DE = h required covers a large
spectral range ; no typical
resonance
I
o
of energy
h

## Slide 43
Intensities of Stokes (filled symbols) and anti-Stokes (open symbols) Raman lines at 1595 cm-1 (G band) measured in a backscattering geometry for semiconducting (~99% pure; up triangles) and metallic (~98% pure; down triangles) of C-SWNTs under 676.4 nm excitation light focused through a 50x microscope objective. The samples were in the form of thin films layered on a glass (triangles) substrate or Ag SERS supports (stars). The Raman intensity was normalized to the signal measured at the lowest excitation intensity (0.2 mW).
Variation with temperature of the IaS/IS ratio associated with the Raman G band (1590 cm-1) for semiconducting (~99% pure, red symbols) and metallic (~98% pure, blue symbols) of C-SWNTs deposited on a glass substrate. All data were obtained at exc = 676.4 nm with 2 mW of laser power focused on the sample through a 50x microscope objective. The green line illustrates the variation allowed by applying the Boltzmann law to the recorded Stokes Raman spectra for metallic tubes.
Variation with excitation laser intensity and temperature of the anti-Stokes
Raman G band of semiconductor and metallic carbon nanotubes
Typical non-linear
dependence for
a non-linear optical process
SRS

## Slide 44
Anti-Stokes and Stokes Raman spectra for semiconductor (~99% pure; S1,S2; black curve) and metallic (~98% pure; M1,M2; red curve) C-SWNTs excited at exc = 676.4 nm with light polarized along (LO) and perpendicular (TO) to the tubes’ axes.
Anti-Stokes Raman intensity of the Raman G band for semiconductor (~99% pure; a) and metallic (~98% pure; b) SWNTs on a Ag support versus the intensity of excitation laser light. All data were obtained at exc = 676.4 nm with light polarized along (LO) and perpendicular (TO) to the tubes’ axes.
Polarized Raman spectra of isolated
semiconducting and metallic nanotubes

## Slide 45
Conclusion:
i) SERS effect manifests differently under non-resonant and resonant optical excitations, it
results from the coupling of plasmons associated with the incident light with the plasmons
associated with the Stokes and anti-Stokes spontaneous Raman emissions.
ii) Under non-resonant and resonant optical excitation SERS manifests as stimulated Raman
process and CARS effect, respectively.
iii) Contrary to the results reported so far , and regardless of whether the optical excitation was
non-resonant or resonant and regardless of whether glass, Au or Ag was used as the substrate,
the metallic single wall carbon nanotubes (SWNTs) do not show an anomalous anti-Stokes
Raman emission.
iv) Semiconducting SWNTs always show an anomalous anti-Stokes Raman emission that grows
further under increases in the excitation light intensity or temperature.
v) Semiconducting SWNTs behave differently than metallic SWNTs because of the splitting
of electronic levels into a vibration structure, which under resonant optical excitation
changes the polarizability of the material by overpopulating the states and contributes
to an enhancement of the anti-Stokes Raman emission;
vi) Metallic SWNTs (like any metal) are infinitely polarizable at very short distances, fact
which determines the invariance of the Stokes Raman spectrum under changes of
the polarization of the excitation light

## Slide 46
Own contributions:
Appl Phys Lett 66,1187-1190,(1995) J Opt Soc Am B 13, 656-660, (1996)
Pure Appl. Opt. 5 , 645–653,(1996) J. Raman Spectrosc. 29, 825È832 (1998)
Phys Rev B 65, 235401,(2002) Carbon, 40,2201-2211,(2002)
J. Opt. A: Pure Appl. Opt. 7,632–639,(2005) Phys. Rev. B,72,(24), 245402-245413,(2005)
Carbon, 43,1-9,(2005) J Raman Spectrosc 36,676-698, (2005)
Physica E: 40(7),2380,(2008) J. Phys:Condensed Matter. 20,(27), 275215, (2008)
Physica status solidi (b) 245, (10), 2221, (2008) Carbon ,47, (5),1389-1398,(2009)
Synthetic Metals 159 , 2173,(2009) J Raman Spectrosc ,42,(3),303, (2011 )
J. Phys. B: At. Mol. Opt. Phys. 44,095401, (2011) Optical materials, 33, (9), 1410,(2011)
J Appl Phy, 110, 053106, (2011) Proc. Romanian Acad., Series A, 13, (2), 109–117, (2012)
J Phys Chem. C, 116, 25537−25545, (2012) Optics Communication : submitted, (2013)
J Raman Spectrosc, submitted, 2013 Journal of Optics : submitted, (2013)

## Slide 47
Use the checkboxes below to view the records. You can choose to view those selected records, or you can exclude them (and view the others). |  |  |  |  | 
 | Field: Authors | Record Count | % of 8993 | Bar Chart | Data rows displayed in table All data rows
1 | DRESSELHAUS MS | 236 | 2.624 % |  | 
2 | SAITO R | 146 | 1.623 % |  | 
3 | JORIO A | 127 | 1.412 % |  | 
4 | DRESSELHAUS G | 122 | 1.357 % |  | 
5 | KATAURA H | 117 | 1.301 % |  | 
6 | KUZMANY H | 113 | 1.257 % |  | 
7 | LEFRANT S | 94 | 1.045 % |  | 
8 | PIMENTA MA | 94 | 1.045 % |  | 
9 | THOMSEN C | 94 | 1.045 % |  | 
10 | IIJIMA S | 76 | 0.845 % |  | 
11 | KAVAN L | 75 | 0.834 % |  | 
12 | ROTH S | 74 | 0.823 % |  | 
13 | SOUZA AG | 71 | 0.790 % |  | 
14 | ENDO M | 69 | 0.767 % |  | 
15 | PICHLER T | 68 | 0.756 % |  | 
16 | BAIBARAC M | 65 | 0.723 % |  | 
17 | BALTOG I | 65 | 0.723 % |  | 
18 | DUNSCH L | 64 | 0.712 % |  | 
19 | SAUVAJOL JL | 64 | 0.712 % |  | 
20 | KIM YA | 61 | 0.678 % |  | 
WEB of Science
2000-2012
9,089 records. Topic = (Raman carbon nanotubes)

## Slide 48
Thanks for your attention

## Slide 49
Carbon allotropic particles
Graphite
Diamond
Fullerene : C60
Graphene
Single wall carbon nanotubes
Multi-wall carbon
nanotubes
metallic
semiconductor
metallic

## Slide 50
What is the wavelength of the surface plasmon ?
let us find k:
substitute
k
w
kx
light cone  = c k
The surface plasmone mode always lies beyond the light line, that is it has greater momentum than a free photon of the same frequency 